20 mm

10 µm

Spc_002

Sem_SED_015

amostra 1

| Items | Value |
| --- | --- |
| measurement conditions |  |
| Acceleration voltage | 15.00 kV |
| Probe current | - |
| Magnification | x 1700 |
| Process time | T3 |
| Measurement detector | First |
| Live time | 30.00 seconds |
| Real time | 41.62 seconds |
| Dead time | 27.00 % |
| Count rate | 69990.00 CPS |

| Display name | Standard data | Quantification method | Result Type |
| --- | --- | --- | --- |
| Spc_002 | Standardless | ZAF | Metal |

| Element | Line | Mass% | Atom% |
| --- | --- | --- | --- |
| C | K | 27.02±0.14 | 45.42±0.23 |
| O | K | 4.77±0.05 | 6.02±0.06 |
| Al | K | 0.57±0.01 | 0.43±0.01 |
| Si | K | 65.84±0.10 | 47.32±0.07 |
| P | K | 0.51±0.01 | 0.33±0.01 |
| Ca | K | 0.52±0.02 | 0.26±0.01 |
| Fe | K | 0.41±0.02 | 0.15±0.01 |
| Zn | K | 0.15±0.04 | 0.05±0.01 |
| As | L | 0.02±0.01 | 0.01±0.00 |
| Cd | L | nd | nd |
| Pb | M | 0.18±0.03 | 0.02±0.00 |
| Total |  | 100.00 | 100.00 |
| Spc_002 |  | Fitting ratio 0.0247 |  |

Signal SED

Landing Voltage 15.0 kV

WD 10.3 mm

Magnification x1,700

Vacuum Mode HighVacuum

Sem_SED_015

28-11 Marina Paiva Abucafy

20 mm

10 µm

Spc_001

Sem_SED_015

amostra 1

| Items | Value |
| --- | --- |
| measurement conditions |  |
| Acceleration voltage | 15.00 kV |
| Probe current | - |
| Magnification | x 1300 |
| Process time | T3 |
| Measurement detector | First |
| Live time | 30.00 seconds |
| Real time | 42.62 seconds |
| Dead time | 29.00 % |
| Count rate | 76385.00 CPS |

| Display name | Standard data | Quantification method | Result Type |
| --- | --- | --- | --- |
| Spc_001 | Standardless | ZAF | Metal |

| Element | Line | Mass% | Atom% |
| --- | --- | --- | --- |
| C | K | 24.32±0.12 | 41.22±0.21 |
| O | K | 8.40±0.06 | 10.69±0.08 |
| Na | K | 0.18±0.01 | 0.16±0.01 |
| Al | K | 0.98±0.01 | 0.74±0.01 |
| Si | K | 63.29±0.09 | 45.88±0.07 |
| P | K | 0.65±0.01 | 0.43±0.01 |
| Ca | K | 0.92±0.02 | 0.47±0.01 |
| Fe | K | 1.06±0.03 | 0.38±0.01 |
| Zn | K | 0.08±0.03 | 0.02±0.01 |
| As | L | 0.01±0.01 | 0.00±0.00 |
| Cd | L | nd | nd |
| Pb | M | 0.13±0.03 | 0.01±0.00 |
| Total |  | 100.00 | 100.00 |
| Spc_001 |  | Fitting ratio 0.0264 |  |

Signal SED

Landing Voltage 15.0 kV

WD 10.3 mm

Magnification x1,300

Vacuum Mode HighVacuum

Sem_SED_015

28-11 Marina Paiva Abucafy

20 mm

50 µm

Spc_002

Sem_SED_029

amostra 2

| Items | Value |
| --- | --- |
| measurement conditions |  |
| Acceleration voltage | 15.00 kV |
| Probe current | - |
| Magnification | x 270 |
| Process time | T3 |
| Measurement detector | First |
| Live time | 30.00 seconds |
| Real time | 35.38 seconds |
| Dead time | 15.00 % |
| Count rate | 35134.00 CPS |

| Display name | Standard data | Quantification method | Result Type |
| --- | --- | --- | --- |
| Spc_002 | Standardless | ZAF | Metal |

| Element | Line | Mass% | Atom% |
| --- | --- | --- | --- |
| C | K | 10.86±0.06 | 23.93±0.13 |
| O | K | 22.88±0.09 | 37.84±0.15 |
| Mg | K | 0.18±0.01 | 0.19±0.01 |
| Al | K | 0.97±0.02 | 0.95±0.02 |
| Si | K | 12.25±0.06 | 11.54±0.05 |
| P | K | 0.50±0.01 | 0.42±0.01 |
| S | K | 0.21±0.01 | 0.17±0.01 |
| Cl | K | 0.53±0.01 | 0.40±0.01 |
| Ca | K | 0.77±0.02 | 0.51±0.01 |
| Fe | K | 50.72±0.23 | 24.03±0.11 |
| Zn | K | nd | nd |
| As | L | nd | nd |
| Cd | L | 0.13±0.02 | 0.03±0.01 |
| Pb | M | 0.03±0.03 | 0.00±0.00 |
| Total |  | 100.00 | 100.00 |
| Spc_002 |  | Fitting ratio 0.0397 |  |

Signal SED

Landing Voltage 15.0 kV

WD 10.1 mm

Magnification x270

Vacuum Mode HighVacuum

Sem_SED_029

28-11 Marina Paiva Abucafy

Pb-M

Cd-L

As-L

Zn-K

Fe-K

Si-K

O-K

IMG1

IMG1(1st)

amostra 2

Pb-M

Cd-L

As-L

Zn-K

Fe-K

Si-K

C-K

IMG1

IMG1(1st)

amostra 1

20 mm

100 µm

Spc_006

Sem_SED_033

amostra 3

| Items | Value |
| --- | --- |
| measurement conditions |  |
| Acceleration voltage | 15.00 kV |
| Probe current | - |
| Magnification | x 170 |
| Process time | T3 |
| Measurement detector | First |
| Live time | 30.00 seconds |
| Real time | 37.60 seconds |
| Dead time | 19.00 % |
| Count rate | 51203.00 CPS |

| Display name | Standard data | Quantification method | Result Type |
| --- | --- | --- | --- |
| Spc_006 | Standardless | ZAF | Metal |

| Element | Line | Mass% | Atom% |
| --- | --- | --- | --- |
| C | K | 47.13±0.12 | 63.05±0.17 |
| O | K | 16.48±0.09 | 16.54±0.09 |
| Al | K | 0.57±0.01 | 0.34±0.01 |
| Si | K | 33.46±0.07 | 19.14±0.04 |
| P | K | 0.58±0.01 | 0.30±0.01 |
| S | K | 0.14±0.01 | 0.07±0.00 |
| Ca | K | 0.73±0.02 | 0.29±0.01 |
| Fe | K | 0.88±0.03 | 0.25±0.01 |
| Zn | K | nd | nd |
| As | L | 0.02±0.01 | 0.00±0.00 |
| Cd | L | nd | nd |
| Pb | M | nd | nd |
| Total |  | 100.00 | 100.00 |
| Spc_006 |  | Fitting ratio 0.0569 |  |

Signal SED

Landing Voltage 15.0 kV

WD 9.9 mm

Magnification x170

Vacuum Mode HighVacuum

Sem_SED_033

28-11 Marina Paiva Abucafy

20 mm

50 µm

Spc_007

Sem_SED_035

amostra 3

| Items | Value |
| --- | --- |
| measurement conditions |  |
| Acceleration voltage | 15.00 kV |
| Probe current | - |
| Magnification | x 430 |
| Process time | T3 |
| Measurement detector | First |
| Live time | 30.00 seconds |
| Real time | 38.81 seconds |
| Dead time | 23.00 % |
| Count rate | 57870.00 CPS |

| Display name | Standard data | Quantification method | Result Type |
| --- | --- | --- | --- |
| Spc_007 | Standardless | ZAF | Metal |

| Element | Line | Mass% | Atom% |
| --- | --- | --- | --- |
| C | K | 46.90±0.12 | 63.21±0.16 |
| O | K | 15.48±0.08 | 15.66±0.09 |
| Al | K | 0.54±0.01 | 0.33±0.01 |
| Si | K | 34.55±0.07 | 19.91±0.04 |
| P | K | 0.49±0.01 | 0.26±0.01 |
| Ca | K | 0.71±0.01 | 0.29±0.01 |
| Fe | K | 1.10±0.03 | 0.32±0.01 |
| Zn | K | 0.03±0.03 | 0.01±0.01 |
| As | L | 0.02±0.01 | 0.00±0.00 |
| Cd | L | 0.02±0.01 | 0.00±0.00 |
| Pb | M | 0.16±0.02 | 0.01±0.00 |
| Total |  | 100.00 | 100.00 |
| Spc_007 |  | Fitting ratio 0.0544 |  |

Signal SED

Landing Voltage 15.0 kV

WD 10.0 mm

Magnification x430

Vacuum Mode HighVacuum

Sem_SED_035

28-11 Marina Paiva Abucafy

Pb-M

Cd-L

As-L

Zn-K

Fe-K

Ca-K

Si-K

Al-K

O-K

C-K

IMG1

IMG1(1st)

amostra 3