## Slide 1
Sem_SED_015
Spc_002
Element | Line | Mass% | Atom%
C | K | 27.02±0.14 | 45.42±0.23
O | K | 4.77±0.05 | 6.02±0.06
Al | K | 0.57±0.01 | 0.43±0.01
Si | K | 65.84±0.10 | 47.32±0.07
P | K | 0.51±0.01 | 0.33±0.01
Ca | K | 0.52±0.02 | 0.26±0.01
Fe | K | 0.41±0.02 | 0.15±0.01
Zn | K | 0.15±0.04 | 0.05±0.01
As | L | 0.02±0.01 | 0.01±0.00
Cd | L | nd | nd
Pb | M | 0.18±0.03 | 0.02±0.00
Total |  | 100.00 | 100.00
Spc_002 |  | Fitting ratio 0.0247 | 
28-11 Marina Paiva Abucafy
Sem_SED_015
10 µm
20 mm
Signal SED
Landing Voltage 15.0 kV
WD 10.3 mm
Magnification x1,700
Vacuum Mode HighVacuum
Display name | Standard data | Quantification method | Result Type
Spc_002 | Standardless | ZAF | Metal
Items | Value
measurement conditions | 
Acceleration voltage | 15.00 kV
Probe current | -
Magnification | x 1700
Process time | T3
Measurement detector | First
Live time | 30.00 seconds
Real time | 41.62 seconds
Dead time | 27.00 %
Count rate | 69990.00 CPS

## Slide 2
Sem_SED_015
Spc_001
Element | Line | Mass% | Atom%
C | K | 24.32±0.12 | 41.22±0.21
O | K | 8.40±0.06 | 10.69±0.08
Na | K | 0.18±0.01 | 0.16±0.01
Al | K | 0.98±0.01 | 0.74±0.01
Si | K | 63.29±0.09 | 45.88±0.07
P | K | 0.65±0.01 | 0.43±0.01
Ca | K | 0.92±0.02 | 0.47±0.01
Fe | K | 1.06±0.03 | 0.38±0.01
Zn | K | 0.08±0.03 | 0.02±0.01
As | L | 0.01±0.01 | 0.00±0.00
Cd | L | nd | nd
Pb | M | 0.13±0.03 | 0.01±0.00
Total |  | 100.00 | 100.00
Spc_001 |  | Fitting ratio 0.0264 | 
28-11 Marina Paiva Abucafy
Sem_SED_015
10 µm
20 mm
Signal SED
Landing Voltage 15.0 kV
WD 10.3 mm
Magnification x1,300
Vacuum Mode HighVacuum
Display name | Standard data | Quantification method | Result Type
Spc_001 | Standardless | ZAF | Metal
Items | Value
measurement conditions | 
Acceleration voltage | 15.00 kV
Probe current | -
Magnification | x 1300
Process time | T3
Measurement detector | First
Live time | 30.00 seconds
Real time | 42.62 seconds
Dead time | 29.00 %
Count rate | 76385.00 CPS